## Slide 1: Ab-initio MD Simulation of GeTe
Jason Larkin
CHE 24-623

## Slide 2: Outline
What is GeTe
Ab-initio MD
Radial Distribution Function
Results from [3] Liquid
Results from [1] Amorphous
Results from [2] Amorphous and GST

## Slide 3: Papers
[1] J. Akola, R.O. Jones Phys. Rev. Lett. 100, 205502 (2008). (Simulation)
[2] J. Akola, R.O. Jones Phys. Rev. B 76, 235201 (2007). (Simulation)
[3] J.Y. Raty, et al., Phys. Rev. B 65, 115205 (2002). (Experiment and Small Simulation)
[4] K. Hirota, et al., J. Appl. Phys. 82(1), 1997. (Experiment)
[5] D.B. Dove, et al., Appl. Phys. Lett. 16, 3 (1970). (Experiment)
All focus on the structural change from crystal->liquid->amorphous

## Slide 4: I. What is GeTe/PC Materials?
Phase Change Materials: Alloys of Ge, Sb, and Te.
Most Popular: Ge2Sb2Te5
Composed of layers of GeTe and Sb2Te3 with vacancies
+
=
Contrast in Optical/Electrical properties between crystalline and amorphous phases.
Ex: difference in resistance 1K-1M Ohm.
Read/write: liquify, quench to amorphous, heat above re-crystallization T (~50 ns).

## Slide 5: II. Ab-initio MD
Feynman-Hellman Theorem:
Assumption: electrons stay in their ground state as nuclei move.
Most of time (again) in calculating forces, so solving better be fast!
CPMD code:
Flexible: if I want to go from GeTe->GST, simple!
Recipe
Given location of nuclei, species, calculate electronic structure.
Take the (analytic) derivative above.
Move nuclei (with say Verlet integration).
Repeat.
http://www.cpmd.org/

## Slide 6: Computational Details
Calculation [1], [2] run on IBM Blue Gene/L, 512 CPUs for 1 month.
[1] includes 216 atoms in a 18.6 Ang. cube.
[2] includes same, 460 atoms GST.
[3] has only 64 atoms!
[1],[2], NVT, dt=0.003 ps
Do results depend on this difference in quench times? NVE vs. NVT?
The entire read/write cycle takes ~50 ns, good luck…
No force-field potentials exists for these materials, so this is as good as it gets.
5000K
1000K
300K
100K
50 ps
29 ps
115ps
26ps
96ps
219ps , expt.~(1000 ps)
Melt T
[3], Langevin, dt=0.003 ps
-A similar melting cycle, but everything done in 11 ps!!!

## Slide 7: III. Radial Distribution Function
Radial Distribution Function (RDF) gives idea of short-range order for liquid/amorphous:
-McGaughey PhD. Thesis
For LJ system, first peak in RDF very nearly same as FCC. True in general??
For multi-species systems, I can have multiple RDFs (looking at say Ge-Ge, Te-Te only).

## Slide 8: IV. Results from [3]
Liquid phase total RDF shows (much) shorter overall and Ge-Ge bonding than crystal.
Neutron diffraction (expt.) shows similar total RDF (short bonds).
With MD data, we can look at species-species RDFs.
Crystal bond
Ge-Ge and Te-Te
Peak at ~2.7 Ang.

## Slide 9: V. Results from [1]
With atom by atom data, we can decompose RDFs (structure factors) into individual components.
We see that overall and Ge-Ge bonds are much shorter in amorphous. Te-Te is close to crystal bond length.
[5]
[4]
Peak at ~2.6 Ang.
(small diff. between graph and actual).
Peak at ~2.6 Ang.
Crystal bond Ge-Ge and Te-Te

## Slide 10: VI. Results from [2]
Again, shortened Ge-Ge and overall bonds, Te-Te nearly same as crystal.
Results for GST materials show similar trends, shortened overall bonds except Te-Te.
Crystal bond Ge-Ge and Te-Te

## Slide 11: Summary
Ab-initio MD flexible, can simulate many systems accurately.
Very expensive, can (mostly) study bulk-like properties.
GeTe Amorphous/Liquid phase total RDF shows (much) shorter overall bonding than crystal.
This is due (primarily) to Ge-x bonding which prefers tetrahedral. Very difficult to capture this with force-field potential!